SECTION 07620 - SHEET METAL FLASHING AND TRIM

- GENERAL

      - SECTION REQUIREMENTS

        - Submittals:  Product Data, Shop Drawings, and Samples.

- PRODUCTS

      - SHEET METAL

        - Galvanized Steel Sheet:  ASTM A 653/A 653M, G90 (Z275), mill phosphatized where indicated for painting; at least 0.0396 inch (1.0 mm) thick.

      - FLASHING AND TRIM

        - Fabricate sheet metal flashing and trim to comply with recommendations of SMACNA's "Architectural Sheet Metal Manual" that apply to the design, dimensions, metal, and other characteristics of the item indicated.

        - Eave drip, gutter, valley, ridge cap.

        - Coil-coat galvanized steel sheet with 2-coat fluoropolymer Hylar 5000 or Kynar 500 finish.

        - Finish aluminum gutters, downspouts, and similar exposed units with baked-on, white-acrylic shop finish; 1.0-mil (0.025-mm) dry film thickness.

      - ACCESSORIES

        - Solder:  ASTM B 32, Grade Sn50.

        - Solder for Stainless Steel:  ASTM B 32, Grade Sn60.

        - Asphalt Mastic:  SSPC-Paint 12, asbestos free, solvent type.

        - Roofing Cement:  ASTM D 4586, Type I, asbestos free, asphalt based.

- EXECUTION

      - INSTALLATION

        - Comply with SMACNA's "Architectural Sheet Metal Manual."  Allow for thermal expansion; set true to line and level.  Install Work with laps, joints, and seams permanently watertight and weatherproof; conceal fasteners where possible.

          - Roof-Edge Flashings:  Secure metal flashings at roof edges according to FM Loss Prevention Data Sheet 1-49 for specified wind zone.

        - Sealed Joints:  Form nonexpansion, but movable, joints in metal to accommodate elastomeric sealant to comply with SMACNA standards.

        - Fabricate nonmoving seams in sheet metal with flat-lock seams.

          - Clean surfaces to be soldered, removing oils and foreign matter.  Pre-tin edges of sheets to be soldered to a width of 1-1/2 inches (38 mm), unless pre-tinned surface would show in finished Work.

        - Separations:  Separate noncompatible metals or corrosive substrates with a coating of asphalt mastic or other permanent separation.

END OF SECTION 07620