SECTION 08800 - GLAZING

- GENERAL

      - SECTION REQUIREMENTS

        - Submittals: Product Data and 12-inch- (300-mm-) square Samples.

        - Fire-Resistance-Rated Assemblies: Products identical to those tested per NFPA 252 for doors and NFPA 257 for window assemblies; both labeled and listed by UL or another testing and inspecting agency acceptable to authorities having jurisdiction.

        - Safety Glass: Category II materials complying with testing requirements in 16 CFR 1201 and ANSI Z97.1.

        - Comply with written instructions of glass product manufacturers; GANA's "Glazing Manual;" and publications of GANA, AAMA, and SIGMA as applicable to products indicated, unless more stringent requirements are indicated.

        - Insulating-Glass Units: Permanently mark with appropriate certification label of one of the inspecting and testing agencies indicated below:

          - Insulating Glass Certification Council.

          - Associated Laboratories, Inc..

          - National Accreditation and Management Institute.

- PRODUCTS

      - GLASS

        - Float Glass: ASTM C 1036, Type I, Class 2 (tinted, heat absorbing, and light reducing), solar grey, and Quality q3.

        - Heat-Treated Float Glass: ASTM C 1048, Condition [A (uncoated)] [C (coated)], Type I, Class 2 (tinted), solar grey, Quality q3, Kind FT (fully tempered).

        - Mirror Glass: ASTM C 1036, Type 1, Class 1, Quality q1 or q2, silver coated per FS DDM411C, 6.0 mm thick, with edges rounded polished.

          - Safety Glass for Mirrors: Laminated.

      - FABRICATED GLASS PRODUCTS

        - Laminated Glass: Two sheets of 6.0-mm- thick float, with urethane acrylate resin interlayer.  Comply with ASTM C 1172.

        - Sealed Insulating-Glass Units: Preassembled units complying with ASTM E 774 for Class CBA units, with two 6.0-mm- thick sheets of glass separated by a 1/2-inch (12.7-mm)dehydrated space filled with argon.

          - Low-Emissivity Coating: Second surface.

- EXECUTION

      - INSTALLATION

        - Comply with combined recommendations of manufacturers of glass, sealants, gaskets, and other glazing materials, unless more stringent requirements are contained in GANA's "Glazing Manual."

        - Set glass lites in each series with uniform pattern, draw, bow, and similar characteristics.

END OF SECTION 08800