SECTION 07115 - BITUMINOUS DAMPPROOFING

- GENERAL

      - SECTION REQUIREMENTS

        - Submittals:  Product Data.

- PRODUCTS

      - MANUFACTURERS

        - ChemRex Inc.  Sonneborn Building Products Div., Koppers Industries Inc., W.R. Meadows Inc.

      - BITUMINOUS DAMPPROOFING

        - Cold-Applied, Asphalt Emulsion Dampproofing:  Asphalt-based emulsions, trowel grade, ASTM D 1227, Type III or IV.

        - Primer:  Asphalt primer, ASTM D 41.

- EXECUTION

      - PREPARATION

        - Prepare substrate by cleaning, removing projections, filling voids, sealing joints, and as otherwise recommended in dampproofing manufacturer's written instructions.

        - Install cant strips, separate flashings, and corner protection stripping, and prime substrate as recommended in dampproofing manufacturer's written instructions.

      - INSTALLATION

        - Comply with manufacturer's written instructions for methods and rates of dampproofing application, cleaning, and installation of protection course.

        - Apply dampproofing to exterior face of concrete and masonry indicated to receive anchored brick veneer and where indicated on Drawings.

        - Apply [1 or more coats] [2 coats] to produce a dry film thickness of at least 60 mils (1.5 mm), average; 30 mils (0.8 mm), minimum.

        - Install glass fabric reinforcement, embedded in dampproofing, at corners and changes in plane.

END OF SECTION 07115