SECTION 05400 - COLD-FORMED METAL FRAMING

- GENERAL

      - SECTION REQUIREMENTS

        - Structural Performance:  Engineer, fabricate, and erect cold-formed metal framing to withstand live loads indicated within the following limits:

          - Interior Non Load-Bearing Walls:  Lateral deflection of [L/360] .

        - Calculate structural characteristics of cold-formed metal framing according to AISI's "Specification for the Design of Cold-Formed Steel Structural Members."

        - Comply with HUD's "Prescriptive Method for Residential Cold-Formed Metal Framing."

        - Submittals:  Product Data and material certificates

        - Comply with AWS D1.1,"Structural Welding Code--Steel," and AWS D1.3, "Structural Welding Code--Sheet Steel."

        - Protect cold-formed metal framing from corrosion and other damage during delivery, storage, and handling.

- PRODUCTS

      - MATERIALS

Select one or more of grade requirements in paragraph below, or revise to a different grade if necessary, distinguishing locations if multiple grades are required.

        - Galvanized Steel Sheet: ASTM A 653/A 653M, G60 (Z180) zinc coated; structural steel; Grade 33 (Grade 230), Class 1 of grade required by structural performance.

        - Steel Studs and Track:  Fabricate with flange width of 1-5/8 inches (41 mm), minimum uncoated steel thickness of 0.0428 inch (1.09 mm), and of depths indicated.

      - ACCESSORIES

        - Steel Shapes and Clips:  ASTM A 36/A 36M, hot-dip galvanized according to ASTM A 153/A 153M

        - Cast-in-Place Anchor Bolts and Studs:  ASTM A 307, Grade A (ASTM F 568, Property Class 4.6); carbon-steel hex-head bolts and studs; carbon-steel nuts; and flat, unhardened-steel washers.  Hot-dip galvanize according to ASTM A 153/A 153M.

        - Mechanical Fasteners:  Corrosion-resistant coated, self-drilling, self-threading steel drill screws.

        - Insulation:  ASTM C 665, Type I, unfaced mineral-fiber blankets.

        - Galvanizing Repair Paint:  SSPC-Paint 20 or DOD-P-21035.

- EXECUTION

      - FRAMING

        - Install framing and accessories level, plumb, square, and true to line, and securely fasten. Temporarily brace framing until entire integrated supporting structure has been completed and permanent connections are secured.

        - Fasten framing members by welding or screw fastening.

        - Install insulation in built-up exterior framing members.

        - Fasten reinforcement plates over web penetrations larger than standard punched openings.

        - Studs:  Install, align, and securely anchor continuous tracks to supporting structure.  Squarely seat studs against webs of top and bottom tracks.  Space studs as indicated; plumb, align, and fasten both flanges of studs to top and bottom track.

          - Install and fasten horizontal bridging in stud system, spaced in rows not more than 48 inches (1219 mm) apart.

          - Install miscellaneous connections, accessories, and supplementary framing.

        - Joists: Install, align, and securely anchor perimeter joist track.  Install joists bearing on supporting framing, level, straight, and plumb, adjust to final position, brace, and reinforce.  Fasten joists to both flanges of joist track.

          - Install bridging and fasten bridging at each joist intersection.

          - Install miscellaneous joist framing and connections, including web stiffeners, closure pieces, clip angles, continuous angles, hold-down angles, anchors, and fasteners.

END OF SECTION 05400