SECTION 02300 - EARTHWORK

- GENERAL

      - SECTION REQUIREMENTS

        - Unauthorized excavation consists of removing materials beyond indicated subgrade elevations or dimensions without direction by Architect.  Unauthorized excavation and remedial work shall be at Contractor's expense.

        - Do not interrupt existing utilities serving facilities occupied by Owner.  Provide temporary utility services.

- PRODUCTS

      - MATERIALS

        - Satisfactory Soil:  ASTM D 2487 Soil Classification Groups GW, GP, GM, SW, SP, and SM; free of rock or gravel larger than 2 inches (50 mm) in any dimension, debris, waste, frozen materials, vegetation, or other deleterious matter.

        - Unsatisfactory Soil:  ASTM D 2487 Soil Classification Groups GC, SC, ML, MH, CL, CH, OL, OH, and PT.

        - Backfill and Fill:  Satisfactory soil materials.

        - Subbase:  Naturally or artificially graded mixture of natural or crushed gravel, crushed stone, and natural or crushed sand, ASTM D 2940, with at least 95 percent passing a 1-1/2-inch (38-mm) sieve and not more than 8 percent passing a No. 200 (0.075-mm) sieve.

        - Bedding:  Subbase materials with 100 percent passing a 1-inch (25-mm) sieve and not more than 8 percent passing a No. 200 (0.075-mm) sieve.

        - Drainage Fill:  Washed, evenly graded mixture of crushed stone, or crushed or uncrushed gravel, ASTM D 448, Size 57, with 100 percent passing a 1-1/2-inch (38-mm) sieve and not more than 5 percent passing a No. 8 (2.36-mm) sieve.

- EXECUTION

      - EARTHWORK

        - Protect subgrades and foundation soils from softening and damage by water, freezing temperatures, or frost.

        - Explosives:  Do not use explosives

        - Excavate to subgrade elevations regardless of character of materials and obstructions encountered.

        - Excavate for structures, building slabs, pavements, and walkways.  Trim subgrades to required lines and grades.

        - Utility Trenches:  Excavate trenches to indicated slopes, lines, depths, and invert elevations. Maintain 12 inches (300 mm) of working clearance on each side of pipe or conduit.

          - Place, compact, and shape bedding course to provide continuous support for pipes and conduits over rock and other unyielding bearing surfaces and to fill unauthorized excavations.

          - Place and compact initial backfill of satisfactory soil material or subbase material, free of particles larger than 1 inch (25 mm), to a height of 12 inches (300 mm) over the utility pipe or conduit.  Place and compact final backfill of satisfactory soil material to final subgrade.

        - Plow strip or break up sloped surfaces steeper than 1 vertical to 4 horizontal to receive fill.

        - When subgrade or existing ground surface to receive fill has a density less than that required for fill, break up ground surface, pulverize, moisture-condition or aerate soil, and recompact.

        - Place backfill and fill in layers not more than 8 inches (200 mm) in loose depth at optimum moisture content.  Compact each layer under structures, building slabs, pavements, and walkways to 95 percent of maximum dry unit weight according to ASTM D 698; elsewhere to 90 percent.

        - Grade areas to a smooth surface to cross sections, lines, and elevations indicated.  Grade lawns, walkways, and unpaved subgrades to tolerances of plus or minus 1-1/4 inch (32 mm) and pavements and areas within building lines to plus or minus 1/2 inch (13 mm).

        - Under pavements and walkways, place subbase course material on prepared subgrades and compact at optimum moisture content to required grades, lines, cross sections, and thicknesses.

        - Under slabs-on-grade, place drainage fill on prepared subgrade and compact to required cross section and thickness.

        - Allow testing agency to inspect and test each subgrade and each fill or backfill layer and verify compliance with requirements.

        - Remove surplus satisfactory soil and waste material, including unsatisfactory soil, trash, and debris, and legally dispose of it off Owner's property.

END OF SECTION 02300