SECTION 05500 - METAL FABRICATIONS

- GENERAL

      - SECTION REQUIREMENTS

        - Submittals:  Shop Drawings showing details of fabrication and installation.

- PRODUCTS

      - METALS

        - Steel Plates, Shapes, and Bars:  ASTM A 36/A 36M.

        - Stainless-Steel Sheet, Strip, Plate, and Flat Bars:  ASTM A 666, Type 304.

        - Rolled Steel Floor Plate:  ASTM A 786/A 786M.

        - Steel Tubing:  Cold-formed steel tubing complying with ASTM A 500.

        - Steel Pipe:  ASTM A 53, standard weight (Schedule 40), black finish.

        - Slotted Channel Framing:  Cold-formed steel channels, 1-5/8 by 1-5/8 inches (41 by 41 mm) by [0.0528-inch (1.35-mm)] [0.0677-inch (1.7-mm)] [0.0966-inch (2.5-mm)] thick with 9/16-inch- (14.3-mm-) wide slotted holes in webs at 2 inches (51 mm) o.c.

        - Iron Castings:  ASTM A 47, Grade 32510 (ASTM A 47M, Grade 22010) or ASTM A 48, Class 30 (ASTM A 48M, Class 200).

        - Aluminum Extrusions:  ASTM B 221 (ASTM B 221M), alloy 6063-T6.

        - Aluminum-Alloy Rolled Tread Plate:  ASTM B 632 (ASTM B 632M) Pattern 1, alloy 6061-T6.

      - GROUT

        - Nonshrink, Nonmetallic Grout:  ASTM C 1107; recommended by manufacturer for exterior applications.

      - FABRICATION

        - General:  Shear and punch metals cleanly and accurately.  Remove burrs and ease exposed edges.  Form bent-metal corners to smallest radius possible without impairing work.

        - Welding:  Weld corners and seams continuously.  Use materials and methods that minimize distortion and develop strength and corrosion resistance of base metals.  At exposed connections, finish welds and surfaces smooth with contour of welded surface matching those adjacent.

        - Fabricate structural-steel door frames from structural shapes and bars fully welded together, with 5/8-by-1-1/2-inch (16-by-38-mm) steel channel stops.  Plug-weld built-up members and continuously weld exposed joints.

          - Provide steel strap anchors, 1/8-by-2-inch (3-by-50-mm) with 8-inch (200-mm) embedment, welded to jambs 12 inches (300 mm) from bottom and head and spaced 30 inches (750 mm) apart.

      - STEEL AND IRON FINISHES

        - Hot-dip galvanize steel fabrications at exterior locations.

        - Prepare uncoated ferrous metal surfaces to comply with SSPC-SP 3, "Power Tool Cleaning," and paint with a rust-inhibitive primer complying with performance requirements of FS TT-P-664.

- EXECUTION

      - INSTALLATION

        - Perform cutting, drilling, and fitting required for installing miscellaneous metal fabrications.  Set metal fabrication accurately in location, alignment, and elevation; with edges and surfaces level, plumb, true, and free of rack.

        - Fit exposed connections accurately together to form hairline joints.

        - Coat concealed surfaces of aluminum that will come into contact with grout, concrete, masonry, wood, or dissimilar metals with a heavy coat of bituminous paint.

END OF SECTION 05500