SECTION 06100 - ROUGH CARPENTRY

- GENERAL

      - SECTION REQUIREMENTS

        - Submittals:  Model code evaluation reports for engineered wood products,

- PRODUCTS

      - LUMBER, GENERAL

        - Dressed lumber, S4S, 15 percent maximum moisture content for 2-inch (38-mm) thickness or less, marked with grade stamp of inspection agency.

      - TREATED MATERIALS

        - Preservative-Treated Materials:  AWPA C2 lumber and AWPA C9 plywood, labeled by an inspection agency approved by ALSC's Board of Review.  After treatment, kiln-dry lumber and plywood to 19 and 15 percent moisture content, respectively.  Treat indicated items and the following:

          - Wood members in connection with roofing, flashing, vapor barriers, and waterproofing.

          - Concealed members in contact with masonry or concrete.

          - Wood framing members less than 18 inches (460 mm) above grade.

          - Wood floor plates installed over concrete slabs directly in contact with earth.

        - Fire-Retardant-Treated Materials:  AWPA C20 lumber and AWPA C27 plywood, interior Type A treatment, labeled by a testing and inspecting agency acceptable to authorities having jurisdiction.

          - Use treated lumber and plywood with bending strength, stiffness, and fastener-holding capacities that are not reduced below values published by manufacturer of chemical formulation under elevated temperature and humidity conditions.

      - LUMBER

        - Dimension Lumber:  The following grades per inspection agency indicated.

          - Non-Load-Bearing Interior Partitions:  Construction, Stud, or No. 2.

          - Framing Other Than Non-Load-Bearing Partitions:  No. 2.

          - Exposed Framing:  Select Structural No. 2, hand selected:

        - Concealed Boards:  19 percent maximum moisture content: Mixed southern pine:  No. 2 per SPIB rules.

        - Miscellaneous Lumber:  No. 3 or Standard grade of any species for nailers, blocking, and similar members.

      - ENGINEERED WOOD PRODUCTS

        - Engineered wood products acceptable to authorities having jurisdiction and with allowable design stresses, as published by manufacturer, that meet or exceed those indicated.  Manufacturer's published values shall be demonstrated by comprehensive testing.

        - Laminated-Veneer Lumber:  Laminated with an exterior-type adhesive complying with ASTM D 2559, with grain of veneers parallel to their lengths.

          - Extreme Fiber Stress in Bending:  2500 psi (17 MPa) for 12-inch nominal- (286-mm actual-) depth members.

          - Modulus of Elasticity:  2,000,000 psi (13 800 MPa).

        - Parallel-Strand Lumber:  Laid up from wood strands with exterior-type adhesive complying with ASTM D 2559,with grain of strands parallel to their lengths.

          - Extreme Fiber Stress in Bending:  2900 psi (20 MPa) for 12-inch nominal- (286-mm actual-) depth members.

          - Modulus of Elasticity:  2,000,000 psi (13 800 MPa).

        - Prefabricated Wood I-Joists:  Made from stress-graded lumber flanges and wood-based structural-use panel webs with exterior-type adhesive complying with ASTM D 2559.

          - Structural Capacities:  Establish and monitor structural capacities according to ASTM D 5055.

      - PANEL PRODUCTS

        - Wood-Based Structural-Use Panels:  DOC PS 2.  Provide plywood complying with DOC PS 1, where plywood is indicated.

          - Factory mark panels evidencing compliance with grade requirements.

          - Provide panels with span ratings required by support spacing indicated.

          - Roof Sheathing:  APA-rated Structural I sheathing, Exterior.

        - Particleboard underlayment:  ANSI A208.1, Grade PBU.

        - Hardboard Underlayment:  ANSI/AHA A135.4, Class 4 (Service), S1S; with back side sanded.

        - Fiberboard Sheathing:  ANSI/AHA A194.1, Type IV, Class 1, 1/2 inch (13 mm) thick.

        - Gypsum Sheathing Board:  ASTM C 79, water-resistant core.

        - Glass-Fiber-Surfaced Gypsum Sheathing Board:  ASTM C 79, water-resistant core, surfaced on face and back with glass-fiber mats with alkali-resistant coating.

        - Extruded Cellular Polystyrene Sheathing:  ASTM C 578, Type IV, with T & G or shiplap long edges.

        - Polyisocyanurate Foam Sheathing:  ASTM C 1289, Type I, Class 2; with aluminum foil facings.  Foam-plastic core and facings shall have flame spread of 25 or less, when tested individually.

      - MISCELLANEOUS PRODUCTS

        - Air-Infiltration Barrier: Polyolefin material complying with ASTM E 1677, Type I, with minimum water-vapor transmission of 10 perms (575 ng/Pa x s x sq. m).

        - Fasteners:  Size and type indicated.  Where rough carpentry is exposed to weather, in ground contact, or in area of high relative humidity, provide fasteners with a hot-dip zinc coating per ASTM A 153 or of Type 304 stainless steel.

          - Power-Driven Fasteners:  CABO NER-272.

          - Bolts:  Steel bolts complying with ASTM A 307, Grade A (ASTM F 568, Property Class 4.6); with ASTM A 563 (ASTM A 563M) hex nuts and, where indicated, flat washers.

        - Metal Framing Anchors:  Hot-dip galvanized steel of structural capacity, type, and size indicated.

        - Sill-Sealer:  Glass-fiber insulation, 1-inch (25-mm) thick, compressible to 1/32 inch (0.8 mm).

        - Adhesives for Field Gluing Panels to Framing:  APA AFG-01.

- EXECUTION

      - INSTALLATION

        - Fit rough carpentry to other construction; scribe and cope for accurate fit.  Correlate location of furring, blocking, and similar supports to allow attachment of other construction.

        - Securely attach rough carpentry work to substrate by anchoring and fastening as indicated, complying with the following:

          - CABO NER-272 for power-driven staples, P-nails, and allied fasteners.

          - Published requirements of metal framing anchor manufacturer.

          - Table 23-I-Q--Nailing Schedule" of the Uniform Building Code.

END OF SECTION 06100