SECTION 06176 - METAL-PLATE-CONNECTED WOOD TRUSSES

- GENERAL

      - SECTION REQUIREMENTS

        - Structural Performance:  Engineer, fabricate, and erect metal-plate-connected wood trusses to withstand design loads without exceeding deflection limits of ANSI/TPI 1, "National Design Standard for Metal-Plate-Connected Wood Truss Construction."

        - Submittals:  Product Data, Shop Drawings, and structural analysis data signed and sealed by a qualified professional engineer registered in the state where the Project is located.

        - Engage a fabricator who participates in a recognized quality-assurance program that involves inspection by an independent inspecting and testing agency acceptable to authorities having jurisdiction.

        - Comply with ANSI/TPI 1; TPI HIB, "Commentary and Recommendations for Handling Installing & Bracing Metal Plate Connected Wood Trusses"; and AFPA's "National Design Specification for Wood Construction" and its "Supplement."

- PRODUCTS

      - MATERIALS

        - Dimension Lumber:  Comply with DOC PS 20, "American Softwood Lumber Standard," any species, graded visually or mechanically.

        - Connector Plates:  Structural-quality steel sheet, zinc coated, complying with ASTM A 653, Grade 33, G60 (ASTM A 653M, Grade 230, Z180) coating designation; at least 0.0359 inch (0.91 mm) thick.

        - Fasteners:  Hot-dip galvanized per ASTM A 153 or stainless steel, Type 304 or 316, where exposed to weather or to high relative humidities.  Size and type indicated.

        - Metal Framing Anchors:  Manufactured from hot-dip, zinc-coated steel sheet complying with ASTM A 653, G60 (ASTM A 653M, Z180) coating designation; structural, commercial, or lock-forming quality, as standard with manufacturer for type of anchor indicated.

      - FABRICATION

        - Fabricate wood trusses within manufacturing tolerances of ANSI/TPI 1 and connect truss members by metal connector plates.

- EXECUTION

      - INSTALLATION

        - Install and brace trusses according to recommendations of TPI.  Space trusses as indicated; install plumb, square, and true to line; and securely fasten to supporting construction.

        - Anchor trusses securely at all bearing points using metal framing anchors and fasten securely.

        - Securely connect each truss ply required for forming built-up girder trusses.  Anchor trusses to girder trusses.

        - Install and fasten permanent bracing during truss erection.  Anchor ends of permanent bracing where terminating at walls or beams.

        - Install wood trusses within installation tolerances of ANSI/TPI 1.

        - Do not alter, cut, or remove truss members.

        - Remove and replace wood trusses that are damaged or deficient.

END OF SECTION 06176