SECTION 07210 - BUILDING INSULATION

- GENERAL

      - SECTION REQUIREMENTS

        - Submittals:  Product Data for each type of insulation product specified.

        - Surface-Burning Characteristics:  ASTM E 84, flame-spread ratings of 25 or less and smoke-developed ratings of 450 or less.

- PRODUCTS

      - INSULATION PRODUCTS

        - Polyisocyanurate Board Insulation:  ASTM C 1289, Type I, Class 1 or 2, faced on both sides with aluminum foil.

- As manufactured by Celotex Corporation or equal

        - Medium density spray foam Insulation:  Thermal Resistance (for 1 inch of  materials) (R-value/inch @75 deg F) ASTM C 518: 6.7 hr.sq.ft. degree F/BTU

- Air Permeance (for 1.5 inch of material): ASTM E 283;  <0.02 L/s.m2 @ 75 Pa

- Wator Vapor Transmission (for 1.5 inches of material) ASTM 96; 0.9 perms

- As manufactured by Gold Seal “icynene MD-C 200” or equal All insulation products shall be approved by Clay County Building Official and State Fire Marshall.

      - ACCESSORIES

        - Vapor Retarder:  Polyethylene, 4 mil thick.

        - Eave Ventilation Troughs:  Preformed, rigid fiberboard or plastic sheets designed to fit between roof framing members and to provide cross-ventilation between attic spaces and vented eaves.

- EXECUTION

      - INSTALLATION

        - Install insulation in areas and in thicknesses indicated or required to produce R-values indicated.  Cut and fit tightly around obstructions and fill voids with insulation.

        - Extend vapor retarder to extremities of areas to be protected from vapor transmission.  Secure in place with adhesives or other anchorage.

END OF SECTION 07210