SECTION 09680 - CARPET

- GENERAL

      - SECTION REQUIREMENTS

        - Submittals:  Product Data and color Samples.

        - Comply with CRI 104, Section 6, "Site Conditions."

        - Extra Materials:  Deliver to Owner full-width carpet equal to 5 percent of each type and color carpet installed, packaged with protective covering for storage.

- PRODUCTS

      - CARPET

        - Hollytex, Clear Performance or approved equal

          - Color and Pattern:  To be selected from manufacturers standard colors

        - Yarn:  100% BCF nylon

        - Surface Pile Weight:  28 oz./sq. yd. (g/sq. m) excluding weight of backings.

        - Total Weight:  67.00 oz./sq. yd. (g/sq. m) including weight of backings  for finished carpet.

        - Primary Backing:  Woven Polypropylene.

        - Secondary Backing:  Woven Polypropylene.

        - Gauge:  1/10

        - Average Pile Height:   .140

        - Critical Radiant Flux Classification:  Class I, not less than 0.45 w/sq. cm per ASTM E 648.

        - Carpet Fire Test –Response Characteristics: Provide carpet with the following fire-test-response characteristics as determined by testing identical products per test method indicated below by UL or another testing and inspection agency acceptable to authorities having jurisdiction. Identify carpet with appropriate markings of applicable testing and inspection agency.

- 1. Surface Flamability:  Passes DOC FF1-70

- 2. Flame Spread:  25 or less per ASTM E 648

- 3. Smoke Developed:  450 or less per ASTM E 84

      - CARPET CUSHION

        - Omni Loc GBS (code UA)

- 1. Unitary adhesive composite backing with with attached woven secondary backing.

- EXECUTION

      - INSTALLATION

        - Comply with CRI 104,  Section 8, "Direct Glue-Down."

        - Maintain uniformity of carpet direction and lay of pile.  At doorways, center seams under door in closed position.  Bind or seal cut edges as recommended by carpet manufacturer.

END OF SECTION 09680