SECTION 04810 - UNIT MASONRY ASSEMBLIES

- GENERAL

      - SECTION REQUIREMENTS

        - Allowances:  Furnish face brick under the Face Brick Allowance specified in Division 1 Section "Price and Payment Procedures."

        - Submittals:  Samples for face brick, hollow brick, and colored mortar.

        - Comply with ACI 530.1/ASCE 6/TMS 602.

        - Mockups:  Construct a sample wall panels approximately 48 inches (1200 mm) long by 48 inches (1200 mm) high to demonstrate aesthetic effects and qualities of materials and execution.

- PRODUCTS

      - MASONRY UNITS

        - Concrete Masonry Units:  ASTM C 90; Weight Classification, Normal Weight; Type I, moisture-controlled units.

          - Special shapes for lintels, corners, jambs, sash, control joints, and other special conditions.

          - Square-edged units for outside corners, unless otherwise indicated.

        - Face Brick:  ASTM C 216, Grade MW or SW, Type FBS.

          - Richtex Bricks No. 506 “Old English”   ( Match Existing )

          - Size:  Standard

          - Solid brick with exposed surfaces finished for ends of sills and caps.

          - Special shapes for applications where shapes produced by sawing would result in sawed surfaces being exposed to view.

      - MORTAR AND GROUT

        - Mortar:  ASTM C 270 proportion specification.  Ready-mixed mortar, ASTM C 1142, may be used at Contractor's option.

          - Masonry Cement:  Do not use masonry cement

          - Do not use calcium chloride in mortar.

          - For masonry below grade or in contact with earth, use Type M.

          - For reinforced masonry, use Type S.

          - For exterior, above-grade, load-bearing and non-load-bearing walls and parapet walls; for interior load-bearing walls; for interior non-load-bearing partitions, and for other applications where another type is not indicated, use Type N.

          - Colored Mortar:  For face brick use colored cement or cement-lime mix of color selected.

          - Water-Repellent Additive:  For mortar used with decorative concrete masonry units, use product recommended by manufacturer of units.

        - Grout: with a slump of 8 to 11 inches (200 to 280 mm).

      - REINFORCEMENT, TIES, AND ANCHORS

        - Steel Reinforcing Bars:  ASTM A 615/A 615M, Grade 60 (Grade 400).

        - Joint Reinforcement:  ASTM A 951, mill galvanized at interior walls and hot-dip galvanized at exterior walls

          - Wire Diameter for Side Rods:  W1.7 or 0.148 inch (3.8 mm)

          - Wire Diameter for Cross Rods:  W1.7 or 0.148 inch (3.8 mm)

          - For single-wythe masonry, provide either ladder design or truss design.

          - For multiwythe masonry, provide ladder design with three side rods

        - Rigid Anchors:  Fabricate from steel bars 1-1/2 inches (38 mm) wide by 1/4 inch (6.4 mm) thick by 24 inches (600 mm) long, with ends turned up 2 inches (50 mm) or with cross pins.

        - Veneer Anchors:  Two-piece adjustable masonry veneer anchors that allow vertical or horizontal adjustment but resist tension and compression forces perpendicular to plane of wall, for attachment over sheathing to studs, and acceptable to authorities having jurisdiction.

      - EMBEDDED FLASHING MATERIALS

        - Sheet Metal Flashing: Copper, 10-oz./sq. ft. (3-kg/sq. m) weight or 0.0135 inch (0.3 mm) thick for fully concealed flashing, 16-oz./sq. ft. (5-kg/sq. m) weight or 0.0216 inch (0.5 mm) thick elsewhere.

        - Laminated Flashing:  Copper sheet 5 oz./sq. ft. (1.5 kg/sq. m) bonded with asphalt between 2 layers of glass-fiber cloth.

        - Rubberized Asphalt Sheet Flashing:  Pliable and highly adhesive rubberized asphalt compound, 26 mils (0.7 mm) thick, bonded to a polyethylene film, 4 mils (0.1 mm) thick, to produce an overall thickness of 30 mils (0.8 mm).

      - MISCELLANEOUS MASONRY ACCESSORIES

        - Compressible Filler:  Premolded strips complying with ASTM D 1056, Grade 2A1.

        - Preformed Control-Joint Gaskets:  Designed to fit standard sash block and to maintain lateral stability in masonry wall; made from styrene-butadiene rubber or PVC.

        - Weep Holes: Cotton sash cord, 24 inches (600 mm) long.

        - Loose-Granular Perlite Insulation:  ASTM C 549, Type II or IV.

        - Extruded-Polystyrene Board Insulation:  ASTM C 578, Type IV or X.

        - Polyisocyanurate Board Insulation:  ASTM C 1289, Type I, Class 2; aluminum-foil faced.

        - Job-Mixed Masonry Cleaner:  1/2-cup (0.14-L) tetrasodium polyphosphate and 1/2-cup (0.14-L) laundry detergent dissolved in 1 gal. (4 L) of water.

- EXECUTION

      - INSTALLATION, GENERAL

        - Cut masonry units with saw.  Install with cut surfaces and, where possible, cut edges concealed.

        - Mix units for exposed unit masonry from several pallets or cubes as they are placed to produce uniform blend of colors and textures.

        - Matching Existing Masonry:  Match coursing, bonding, color, and texture of existing masonry.

        - Stopping and Resuming Work:  Rack back units; do not tooth.

        - Fill cores in hollow concrete masonry units with grout 24 inches (600 mm) under bearing plates, beams, lintels, posts, and similar items, unless otherwise indicated.

        - Build non-load-bearing interior partitions full height and install compressible filler in joint between top of partition and underside of structure above.

        - Tool exposed joints slightly concave when thumbprint hard, unless otherwise indicated.

        - Keep cavities clean of mortar droppings and other materials during construction.  Strike joints facing cavities flush.

      - LINTELS

        - Install steel lintels where indicated.

        - Provide masonry lintels where shown.  Use precast lintels made from concrete matching concrete masonry units in color, texture, and compressive strength and with reinforcement bars indicated or required to support loads indicated.

        - Minimum bearing of 8 inches (200 mm) at each jamb, unless otherwise indicated.

      - FLASHING AND WEEP HOLES

        - Install embedded flashing and weep holes in masonry at shelf angles, lintels, ledges, other obstructions to the downward flow of water in the wall, and where indicated.

        - Place through-wall flashing on sloping bed of mortar and cover with mortar.  Seal penetrations in flashing before covering with mortar.

          - Extend flashing 4 inches (100 mm) into masonry at each end and turn up 2 inches (50 mm) to form a pan.

        - Trim wicking material used in weep holes flush with outside face of wall after mortar has set.

      - FIELD QUALITY CONTROL

        - Owner will engage a qualified independent testing agency to perform the following tests for each 5000 sq. ft. (460 sq. m) of wall area or portion thereof.

          - Mortar:  ASTM C 780.

          - Grout:  ASTM C 1019.

          - Brick:  ASTM C 67.

          - Concrete Masonry Units:  ASTM C 140.

      - PARGING

        - Parge predampened masonry walls, where indicated, with Type S or Type N mortar applied in 2 uniform coats with a steel-trowel finish.  Form a wash at top of parging and a cove at bottom.  Damp cure parging for at least 24 hours.

      - CLEANING

        - Clean masonry as work progresses.  Remove mortar fins and smears before tooling joints.

        - Final Cleaning:  After mortar is thoroughly cured, remove large mortar particles, scrub, and rinse unit masonry.

          - Wet wall surfaces with water before applying acidic cleaner, then remove cleaner promptly by rinsing thoroughly with clear water.

END OF SECTION 04810