SECTION 07920 - JOINT SEALANTS

- GENERAL

      - SECTION REQUIREMENTS

        - Submittals: Product Data and color Samples.

- PRODUCTS

      - JOINT SEALANTS

        - Compatibility: Provide joint sealants, joint fillers, and other related materials that are compatible with one another and with joint substrates under service and application conditions.

        - Elastomeric Sealants: Comply with ASTM C 920.

          - Single-component, nonsag polysulfide sealant, Type S; Grade NS; Class 12-1/2; Uses NT, M, G, A, and O.  For general exterior use.

          - Single-component, neutral-curing silicone sealant, Type S; Grade NS; Class 25; Uses T, NT, M, G, A, and O.  For general exterior use.

          - Single-component, nonsag urethane sealant, Type S; Grade NS; Class 25; and Uses NT, M, A, and O.  For general exterior use.

          - Single-component, nonsag urethane sealant, Type S; Grade NS; Class 25; Uses T, NT, M, G, A, and O.  Use for exterior traffic-bearing joints, where slope precludes use of pourable sealant.

          - Single-component, pourable urethane sealant, Type S; Grade P; Class 25; Uses T, M, G, A, and O.  Use for exterior traffic-bearing joints.

          - Single-component, mildew-resistant silicone sealant, Type S; Grade NS; Class 25; Uses NT, G, A, and O; formulated with fungicide.  Use for interior sealant joints in ceramic tile, stone, and other hard surfaces in kitchens and toilet rooms and around plumbing fixtures.

        - Latex Sealant: Single-component, nonsag, mildew-resistant, paintable, acrylic-emulsion sealant complying with ASTM C 834.  For interior use only at perimeters of door and window frames.

- EXECUTION

      - INSTALLATION

        - Comply with ASTM C 1193.

        - Comply with ASTM C 919 for use of joint sealants in acoustical applications.

END OF SECTION 07920