SECTION 03300 - CAST-IN-PLACE CONCRETE

- GENERAL

      - SECTION REQUIREMENTS

        - Submittals:  Product Data, concrete mix designs, laboratory test reports.

        - Comply with ASTM C 94; ACI 301, "Specification for Structural Concrete"; ACI 117, "Specifications for Tolerances for Concrete Construction and Materials"; and CRSI's "Manual of Standard Practice."

        - Engage a qualified independent testing agency to design concrete mixes.

- PRODUCTS

      - MATERIALS

        - Deformed Reinforcing Bars:  ASTM A 615/A 615M, Grade 60 (Grade 420).

        - Plain Steel Wire:  ASTM A 82, as drawn.

        - Steel Welded-Wire Fabric:  ASTM A 185, flat sheets not rolls.

        - Portland Cement:  ASTM C 150, Type I or II.

        - Fly Ash:  ASTM C 618, Type C or F.

        - Aggregates:  ASTM C 33, uniformly graded.

        - Fiber Reinforcement:  ASTM C 1116, Type III, synthetic fibers, 1/2 to 1 inch (13 to 25 mm).

        - Air-Entraining Admixture:  ASTM C 260.

        - Chemical Admixtures:  ASTM C 494, water reducing, high-range water reducing, water reducing and accelerating, and water reducing and retarding].

        - Water Stops:  Flat dumbbell or center-bulb type, of either rubber (CRD C 513) or PVC (CRD C 572)  Self-expanding, hydrophylic, rectangular or trapezoidal strips.

        - Vapor Retarder:  Clear 10-mil- (0.25-mm-) thick polyethylene sheet  Reinforced polyethylene sheet, ASTM E 1745, Class C.

        - Slip-Resistive Aggregate:  Factory-produced, rustproof, nonglazing, fused aluminum-oxide granules or crushed emery, unaffected by freezing, moisture, and cleaning materials.

        - Joint-Filler Strips:  ASTM D 1751, cellulosic fiber, or ASTM D 1752, cork.

        - Repair Underlayment:  Factory-packaged, portland or blended hydraulic cement-based, polymer-modified, self-leveling underlayment with minimum 28-day compressive strength of 4100 psi (29 MPa).

        - Repair Topping:  Factory-packaged, portland or blended hydraulic cement-based, polymer-modified, self-leveling traffic-bearing topping with minimum 28-day compressive strength of 5700 psi (39 MPa).

      - MIXES

        - Proportion normal-weight concrete mixes to provide the following properties:

Select or revise mix properties below to meet Project requirements.  Distinguish locations of each concrete mix if more than one.

          - Compressive Strength:  2500 psi (17.3 MPa)  3000 psi (20.7 MPa)  3500 psi (24.1 MPa)  4000 psi (27.6 MPa)  at 28 days

          - Slump Limit:  4 inches (100 mm).

          - Air Content:  5.5 to 7.0 percent for concrete exposed to freezing and thawing, 2 to 4 percent else

- where.

- 4.

- EXECUTION

      - CONCRETING

        - Construct formwork and maintain tolerances and surface irregularities within ACI 117 limits of Class A for concrete exposed to view and Class C for other concrete surfaces.

        - Set water stops where indicated to ensure joint watertightness.

        - Place vapor retarder on prepared subgrade, with joints lapped 6 inches (150 mm) and sealed.

        - Accurately position, support, and secure reinforcement.

        - Install construction, isolation, and contraction joints where indicated.  Install full-depth joint-filler strips at isolation joints.

        - Place concrete in a continuous operation and consolidate using mechanical vibrating equipment.

        - Protect concrete from physical damage, premature drying, and reduced strength due to hot or cold weather during mixing, placing, and curing.

        - Formed Surface Finish:  Smooth-formed finish for concrete exposed to view, coated, or covered by waterproofing or other direct-applied material; rough-formed finish elsewhere.

        - Slab Finishes:  Scratch finish for surfaces to receive mortar setting beds, Troweled finish for floor surfaces and floors to receive floor coverings, paint, or other thin film-finish coatings, Trowel and fine-broom finish for surfaces to receive thin-set tile, Nonslip-broom finish to exterior concrete platforms, steps, and ramps.

        - Cure formed surfaces by moist curing for at least seven days.

        - Begin curing concrete slabs after finishing.  Keep concrete continuously moist for at least seven days

        - Owner will engage a testing agency to perform field tests and to submit test reports.

        - Protect concrete from damage.  Repair surface defects in formed concrete and slabs.

        - Repair slabs not meeting surface tolerances by grinding high areas and by applying a repair underlayment to low areas receiving floor coverings and a repair topping to low areas to remain exposed.

        - Ready mix concrete:  Comply with ASTM C 94 mixing and delivery time shall not exceed 75 minutes when air temperatures are between 85 an 90 deg F and 60 minutes when air temperatures are above 90 deg F.

END OF SECTION 03300