SECTION 08110 - STEEL DOORS AND FRAMES

- GENERAL

      - SECTION REQUIREMENTS

        - Submittals: Product Data and door schedule.

        - Comply with ANSI/SDI 100.

        - Fire-Rated Door Assemblies: NFPA 80, tested per ASTM E 152, and labeled and listed by UL, ITS, or another testing and inspecting agency acceptable to authorities having jurisdiction.

- PRODUCTS

      - MATERIALS

        - Hot-Rolled Steel Sheets: ASTM A 569/A 569M.

        - Cold-Rolled Steel Sheets: ASTM A 366/A 366M or ASTM A 620/A 620M.

        - Galvanized Steel Sheets: ASTM A 653/A 653M, commercial steel, or ASTM A 642/A 642M, drawing quality, with A60 or G60 (ZF180 or Z180) coating designation, mill phosphatized.

      - STEEL DOORS AND FRAMES

        - Republic or equal

        - Steel Doors: 1-3/4-inch- (44-mm-) thick of materials and ANSI/SDI 100 grades and models specified below.

          - Interior Doors: Grade II, heavy-duty, Model 2, seamless design, minimum 0.0478-inch- (1.2-mm-) thick, cold-rolled steel sheet faces.

          - Exterior Doors: Grade III, extra heavy-duty, Model 2, seamless design, minimum 0.0635-inch- (1.6-mm-) thick, galvanized steel sheet faces.

        - Door Louvers:  Sight-proof per SDI 111C.

          - Fire-Rated Automatic Louvers: Actuated by fusible links at 150 deg F (65 deg C) and listed and labeled.

        - Door Silencers: Three on strike jambs of single-door frames and two on heads of double-door frames.

        - Plaster Guards: Provide where mortar might obstruct hardware operation and to close off interior of openings.

        - Fabricate steel frames to be rigid, neat in appearance, and free from defects, warp, or buckle.

          - Interior Frames: Corners knocked down for field assembly, formed from 0.0478-inch- (1.2-mm-) thick, cold-rolled steel for openings 48 inches (1220 mm) or less in width and from 0.0598-inch- (1.5-mm-) thick steel for openings more than 48 inches (1220 mm) in width.

          - Exterior Frames: Fabricate with mitered or coped and continuously welded corners, formed from 0.0635-inch- (1.6-mm-) thick, galvanized steel sheet.

        - Prepare doors and frames to receive mortised and concealed hardware according to SDI 107.

        - Prime Coat: Uncoated steel, ANSI A224.1 shop primer, galvanized steel, FS TT-P-641, Type II zinc-dust, zinc-oxide primer.

- EXECUTION

      - INSTALLATION

        - Place steel frames to comply with SDI 105.

        - Install steel doors accurately in frames, within clearances specified in ANSI/SDI 100.

          - Fire-Rated Doors: Install with clearances specified in NFPA 80.

          - Smoke-Control Doors: Comply with NFPA 105.

        - Prime Coat Repair: Immediately after erection, sand smooth any rusted or damaged areas of prime coat and repair finish with compatible air-drying primer.

END OF SECTION 08110